1000mm 1/4� Superflexible Cable Jumper

( N Male to N Male Connector )

Connector Interface:  CECC  22190 ;IEC 60169-4 ;DIN 47223

Electrical

Characteristic Impedance                                         50 ohm

Frequency Range                                               DC-3 GHz

VSWR                                                   ≤1.10@698-960MHz

≤1.10@1900-2500MHz

Dielectric Withstanding Voltage                          ≥2500V RMS,50Hz,at sea level

Dielectric Resistance                                             ≥5000MΩ

Mechanical

Durability                                                Mating cycles ≥500

Material and Plating

Material               Plating

Body                        Brass                         Ni

Insulator                     PTFE                       －

Center conductor              Phosphor bronze                  Au

Coupling nut                 Brass                                Ni

Gasket                      Silicone Rubber                       －

Shrinkable Tube               PVC                               －

Cable Family            1/4� Superflexible cable (Made by China Cable manufacturer)

Environmental

Temperature Range                                            -40℃～+85℃al

Weatherproof Rate                                               IP 67

RoHs 2002/95/EC   Compliant

1/4″Super  Flexible  Cable

Construction Specification

|  | Material | Diameter(mm) |
| --- | --- | --- |
| 1. Inner Conductor | Copper Clad Aluminum Wire or Copper | 1.90 |
| 2. Dielectric | Physical Foam Polyethylene | 4.70 |
| 3. Outer Conductor | Helical Copper Tube | 6.35 |
| 4. Jacket | Black PE or Low Smoke Halogen-free Fire-retardant PE | 7.50 |
|  | Material | Diameter(mm) |
| 1. Inner Conductor | Copper Clad Aluminum Wire or Copper | 1.90 |
| 2. Dielectric | Physical Foam Polyethylene | 4.70 |
| 3. Outer Conductor | Helical Copper Tube | 6.35 |
| 4. Jacket | Black PE or Low Smoke Halogen-free Fire-retardant PE | 7.50 |

Electrical Characteristics                          Mechanical and Environmental Characteristics

| Capacitance(pF/m) | 80 |  | Min. Single Bending Radius(mm) | 12.50 |
| --- | --- | --- | --- | --- |
| Impedance(ohm) | 50 |  | Min. Repeated Bending Radius(mm) | 25 |
| Velocity(%) | 83 |  | No. of Bends | 15 |
| Peak Power Rating(KW) | 6.40 |  | Mobile Apply(mm) | 350 |
| RF Peak Voltage(KV) | 0.80 |  | Bending Moment(N.m) | 5.0 |
| Insulation Resistance(MΩ.km) | >5000 |  | Tensile Strength(kg) | 60 |
| Cut-off Frequency(GHz) | 20.4 |  | Storage Temp.(℃) | -55to+85 |
| Insulation Voltage(KV) | 2.0 |  | Installation Temp. (℃) | -40to+60 |
| Inner Conductor DC Resistance(Ω/km) | 9.50 |  | Operating Temp.( ℃) | -55to+85 |
| Outer Conductor DC Resistance(Ω/km) | 5.70 |  |  |  |
| Jacket Spark(KV) | 3.0 |  |  |  |
| Shielding Effectiveness(dB) | >120 |  |  |  |
| VSWR≤(Return loss≥dB) |  |  |  |  |
| 0.005-3GHz | 1.15 | (23) |  |  |  |
| 0.8-1.0GHz | 1.10 | (26) |  |  |  |
| 1.7-2.0GHz | 1.10 | (26) |  |  |  |
| 2.0-2.4GHz | 1.10 | (26) |  |  |  |
| Capacitance(pF/m) | 80 |  | Min. Single Bending Radius(mm) | 12.50 |
| Impedance(ohm) | 50 |  | Min. Repeated Bending Radius(mm) | 25 |
| Velocity(%) | 83 |  | No. of Bends | 15 |
| Peak Power Rating(KW) | 6.40 |  | Mobile Apply(mm) | 350 |
| RF Peak Voltage(KV) | 0.80 |  | Bending Moment(N.m) | 5.0 |
| Insulation Resistance(MΩ.km) | >5000 |  | Tensile Strength(kg) | 60 |
| Cut-off Frequency(GHz) | 20.4 |  | Storage Temp.(℃) | -55to+85 |
| Insulation Voltage(KV) | 2.0 |  | Installation Temp. (℃) | -40to+60 |
| Inner Conductor DC Resistance(Ω/km) | 9.50 |  | Operating Temp.( ℃) | -55to+85 |
| Outer Conductor DC Resistance(Ω/km) | 5.70 |  |  |  |
| Jacket Spark(KV) | 3.0 |  |  |  |
| Shielding Effectiveness(dB) | >120 |  |  |  |
| VSWR≤(Return loss≥dB) |  |  |  |  |
| 0.005-3GHz | 1.15 | (23) |  |  |  |
| 0.8-1.0GHz | 1.10 | (26) |  |  |  |
| 1.7-2.0GHz | 1.10 | (26) |  |  |  |
| 2.0-2.4GHz | 1.10 | (26) |  |  |  |

Attenuation(VSWR1.0,cable temp.20℃) and Average Power(VSWR1.0,ambient temp.40℃)

| Frequency(MHz) | Attenuation(≯dB/100m) | Average Power(KW) |
| --- | --- | --- |
| 100 | 5.60 | 1.23 |
| 200 | 8.00 | 0.86 |
| 450 | 12.20 | 0.57 |
| 800 | 16.70 | 0.42 |
| 900 | 17.50 | 0.39 |
| 1000 | 18.60 | 0.37 |
| 1500 | 23.40 | 0.30 |
| 1800 | 25.70 | 0.27 |
| 2000 | 26.90 | 0.26 |
| 2200 | 28.50 | 0.25 |
| 2400 | 30.00 | 0.24 |
| 2500 | 30.60 | 0.23 |
| 3000 | 33.50 | 0.21 |
| Frequency(MHz) | Attenuation(≯dB/100m) | Average Power(KW) |
| 100 | 5.60 | 1.23 |
| 200 | 8.00 | 0.86 |
| 450 | 12.20 | 0.57 |
| 800 | 16.70 | 0.42 |
| 900 | 17.50 | 0.39 |
| 1000 | 18.60 | 0.37 |
| 1500 | 23.40 | 0.30 |
| 1800 | 25.70 | 0.27 |
| 2000 | 26.90 | 0.26 |
| 2200 | 28.50 | 0.25 |
| 2400 | 30.00 | 0.24 |
| 2500 | 30.60 | 0.23 |
| 3000 | 33.50 | 0.21 |